Table 9. Comparison of results for plate 1600×800×14 mm with 0-20 years of exposure.

|  | Buckling Strength | Ultimate Strength |
| --- | --- | --- |
| Case |  |  |  |  |
| uncorroded | 0.643 | 0 | 0.772 | 0 |
| 5-year exposure | 0.596 | 7.39 | 0.724 | 6.21 |
| 10-year exposure | 0.471 | 26.68 | 0.601 | 22.15 |
| 15-year exposure | 0.280 | 56.45 | 0.535 | 30.67 |
| 20-year exposure | 0.204 | 68.20 | 0.476 | 38.39 |

Table 10. Comparison of results for plate 2400×800×14 mm with 0-20 years of exposure.

|  | Buckling Strength | Ultimate Strength |
| --- | --- | --- |
| Case |  |  |  |  |
| uncorroded | 0.661 | 0 | 0.750 | 0 |
| 5-year exposure | 0.602 | 8.99 | 0.701 | 6.46 |
| 10-year exposure | 0.472 | 28.67 | 0.634 | 15.49 |
| 15-year exposure | 0.348 | 47.38 | 0.575 | 23.27 |
| 20-year exposure | 0.253 | 61.67 | 0.531 | 29.22 |

Table 11. Comparison of results for plate 1600×800×18 mm with 0-20 years of exposure.

|  | Buckling Strength | Ultimate Strength |
| --- | --- | --- |
| Case |  |  |  |  |
| uncorroded | 0.889 | 0 | 0.931 | 0 |
| 5-year exposure | 0.8229 | 7.50 | 0.885 | 4.91 |
| 10-year exposure | 0.7769 | 12.66 | 0.841 | 9.62 |
| 15-year exposure | 0.617 | 30.60 | 0.760 | 18.34 |
| 20-year exposure | 0.475 | 46.50 | 0.632 | 32.13 |

Table 12. Comparison of results for plate 2400×800×18 mm with 0-20 years of exposure.

|  | Buckling Strength | Ultimate Strength |
| --- | --- | --- |
| Case |  |  |  |  |
| uncorroded | 0.872 | 0 | 0.924 | 0 |
| 5-year exposure | 0.811 | 6.94 | 0.887 | 3.93 |
| 10-year exposure | 0.745 | 14.56 | 0.814 | 11.89 |
| 15-year exposure | 0.616 | 29.38 | 0.724 | 21.58 |
| 20-year exposure | 0.511 | 41.38 | 0.661 | 28.47 |

Table 13. A selection of stress distributions and deflection modes for corroded stiffened plate model F3 at ultimate strength level and final step of calculations (magnification factor for deflection mode: 10)

| Plate 24, 2mm Corrosion, S=0.2 mm, NS steel |
| --- |
| Case | Ultimate strength step |  | Final Step |  |
| No Corrosion |  | 0.759 |  | 0.462 |
| Uniform Corrosion |  | 0.678 |  | 0.421 |
| Random Upper Band |  | 0.678 |  | 0.423 |
| Random Lower Band |  | 0.675 |  | 0.358 |

Table 14. A selection of stress distributions and deflection modes for corroded stiffened plate model T3 at ultimate strength level and final step of calculations (magnification factor for deflection mode: 10)

| Plate 24, 2mm Corrosion, S=0.2 mm, NS steel |
| --- |
| Case | Ultimate strength step |  | Final Step |  |
| No Corrosion |  | 0.841 |  | 0.418 |
| Uniform Corrosion |  | 0.764 |  | 0.376 |
| Random Upper Band |  | 0.766 |  | 0.404 |
| Random Lower Band |  | 0.762 |  | 0.377 |

Table 15. A selection of stress distributions and deflection modes for corroded stiffened plate model L3 at ultimate strength level and final step of calculations (magnification factor for deflection mode: 10)

| Plate 24, 2mm Corrosion, S=0.2 mm, NS steel |
| --- |
| Case | Ultimate strength step |  | Final Step |  |
| No Corrosion |  | 0.871 |  | 0.444 |
| Uniform Corrosion |  | 0.795 |  | 0.401 |
| Random Upper Band |  | 0.791 |  | 0.495 |
| Random Lower Band |  | 0.790 |  | 0.398 |